Supplementary Information

Concentration- and Cucurbit[n]urils-Regulated Molecular Packing Modes for Constructing Continuously Red-Shifted Multi-stimuli Responsive Luminescent System

Junli Yang a, Dongdong Sun b, Xingbo Guo a, Ziwei Hu a, Qiandie Yang a, Mengling Lang a, Le Chen a, Zhengfen Liu a, *, and Xianchen Hu a, *

a: College of Chemical and Materials Engineering, Qujing Normal University, Qujing 655011, China.

b: College of Science, Henan Agricultural University, Zhengzhou 450002, China.

* Corresponding authors.

E-mail addresses: hxc413970239@163.com (X. Hu), zhengfen_liu@163.com (Z. Liu)

Table of Contents

Section A. Characterization of Compound………………………………………………………S2

Section B. Host-guest recognition of CB[n] (n = 7, 8, 10) and G1………………………………S5

Section C. The photophysical properties of G1 and the host-guest inclusion complexes………S9

Section D. DFT calculations…………………………………………………………….……… S13

Section A. Characterization of Compound

Figure S1. The 1H NMR spectroscopic spectrum of compound 1-1 (400 MHz, CDCl3, 298 k).

Figure S2. The 1H NMR spectroscopic spectrum of compound 1-2 (400 MHz, D2O, 298 k).

Figure S3. The 1H NMR spectroscopic spectrum of compound G1 (400 MHz, D2O, 298 k).

Figure S4. The 13C NMR spectroscopic spectrum of compound G1 (400 MHz, DMSO-d6, 298 k).

Figure S5. ESI-MS spectrum of G1.

Section B. Host-guest recognition of CB[n] (n = 7, 8, 10) and G1

Figure S6. 1H NMR spectroscopic spectrum of G1 (0.50 mM, 400 MHz, D2O, 298 K) with 1.00 equiv. of CB[7].

Figure S7. 1HNMR spectroscopic titration spectra of G1 (0.50 mM, 400 MHz, D2O, 298 K) with (a) 0.00 equiv., (b) 0.17 equiv., (c) 0.33 equiv., (d) 0.50 equiv. of CB[8]. Characters 1~8 and 1'~8' represent the resonance signals of G1 as free and in CB[8]·G12, respectively.

Figure S8. 1H NMR spectroscopic spectrum of G1 (0.50 mM, 400 MHz, D2O, 298 K) with 0.50 equiv. of CB[8].

Figure S9. NOESY NMR spectrum recorded (600 MHz, D2O, 298 K) for compound CB[8]·G12 ([G1] = 0.50 mM).

Figure S10. 1H NMR spectroscopic titration spectra of G1 (0.50 mM, 400 MHz, D2O, 298 K) with (a) 0.00 equiv., (b) 0.18 equiv., (c) 0.28 equiv., (d) 0.38 equiv., (e) 0.50 equiv. of CB[10]. Characters 1~8 and 1'~8' represent the resonance signals of G1 as free and in CB[10]·G12, respectively.

Figure S11. 1H NMR spectroscopic spectrum of G1 (0.50 mM, 400 MHz, D2O, 298 K) with 0.50 equiv. of CB[10].

ITC spectra of guest G1 and CB[8]

The instrument used in the isothermal titration calorimetry (Nano ITC) was TA Instruments, with a temperature controlled at 298 K.

Figure S12. Isothermal titration calorimetry data for (a) compound G1 with CB[7] in H2O ([G1] (syringe) = 5.0 × 10-4 M, [CB[7]] (cell) = 5.0×10-5 M) and (b) compound G1 with CB[8] in H2O ([G1] (syringe) = 5.0×10-4 M, [CB[8]] (cell) = 5.0×10-5 M).

Section C. The photophysical properties of G1 and the host-guest inclusion complexes

Figure S13. 1H NMR spectroscopic spectra of compound G1 (400 MHz, D2O, 298 K) at different concentrations, (a) 0.10 mM, (b) 0.20 mM, (c) 0.30 mM, (d) 0.40 mM, (e) 0.50 mM.

Figure S14. Normalized emission spectra of G1 in different solvents (298 K, λex = 350 nm, [G1] = 2.0 × 10-5 M).

Figure S15. Normalized UV-Vis absorption spectra of free G1 at different concentrations.

Figure S16. The UV-Vis absorption spectra of G1 (0.02 mM) in the presence of different amount of CB[7] (0.00~1.00 equiv.).

Figure S17. The UV-Vis absorption spectra of G1 (0.02 mM) in the presence of different amount of CB[8] (0.00~0.50 equiv.).

Figure S18. The UV-Vis absorption spectra of G1 (0.02 mM) in the presence of different amount of CB[10] (0.00~0.5 equiv.).

Table S1. Steady-state spectral data of G1, CB[7]·G1, CB[8]·G12, CB[10]·G12.

| Compound | λem (nm) | τ (ns) |
| --- | --- | --- |
| G1（0.02 mM） | 464 | 23.15 |
| G1（0.50 mM） | 490 | 13.15 |
| CB[7]·G1（0.50 mM） | 445 | 8.42 |
| CB[8]·G12（0.50 mM） | 526 | 30.29 |
| CB[10]·G12（0.50 mM） | 546 | 41.18 |

Figure S19. Time-correlated single photon counting decay profiles for G1, CB[7]·G1, CB[8]·G12, CB[10]·G12.

Section D. DFT calculations

Figure S20. Optimized structures of (a) G1, (b) CB[7]·G1, (c) CB[8]·G12, (d) CB[10]·G12.

Table S2 Calculation details of the optimized structures.

| Compound | Energy / Hartree | Dipole Moment / Debye |
| --- | --- | --- |
| G1 | -1421.878539 | 0.098286 |
| Dimer structure of G1 | -2843.807065 | 0.232239 |
| CB[7]·G1 | -5634.715179 | 1.345295 |
| CB[8]·G12 | -7658.520430 | 1.026245 |
| CB[10]·G12 | -8862.087440 | 0.244448 |

Cartesian coordinates of optimized monomer (compound G1), ground state

C                 -0.31160176    0.56553241    0.30399152

C                  0.31136680   -0.56796694   -0.30876759

C                 -0.51015806   -1.57891252   -0.87734151

C                 -1.87767845   -1.48198328   -0.83044658

C                 -2.50736414   -0.35547320   -0.22353456

C                 -1.72239642    0.64642131    0.32789708

C                  0.50987357    1.57651678    0.87255859

C                  1.87739490    1.47952697    0.82581819

C                  2.50706412    0.35292163    0.21909388

C                  1.72216513   -0.64894159   -0.33248958

C                  3.97475124    0.26274767    0.16928092

C                 -3.97504392   -0.26546449   -0.17306442

C                  4.77975544    1.41553548    0.10569425

C                  6.15190216    1.31086844    0.06277461

N                  6.75806179    0.09540454    0.06663858

C                  6.01210825   -1.03878529    0.12235709

C                  4.63858007   -0.97835893    0.18325490

C                 -4.77998653   -1.41833198   -0.11028816

C                 -6.15213035   -1.31378984   -0.06632897

N                 -6.75831881   -0.09836634   -0.06820496

C                 -6.01244068    1.03591243   -0.12346178

C                 -4.63897976    0.97562781   -0.18546403

C                  8.20096463    0.00789514    0.01172873

C                 -8.20111407   -0.00989719   -0.01102920

C                  8.87391257   -0.78056449    0.94361093

C                 10.26220511   -0.86271878    0.87630762

C                 10.98605746   -0.16516997   -0.10048713

C                 10.27767370    0.61756715   -1.02301101

C                  8.88942302    0.70968181   -0.97678114

C                 -8.87478767    0.77763931   -0.94370759

C                -10.26304555    0.85618167   -0.87866244

C                -10.98644625    0.15993697    0.09998530

C                -10.27822108   -0.62755978    1.01797884

C                 -8.88930009   -0.71607791    0.97400843

C                 12.49098173   -0.23541840   -0.14367430

C                -12.48720960    0.27595461    0.17717283

H                 -0.03926421   -2.43258372   -1.35512534

H                 -2.48461839   -2.25391001   -1.29036892

H                 -2.17983134    1.49809392    0.82087653

H                  0.03894453    2.43022461    1.35024144

H                  2.48437907    2.25143281    1.28572401

H                  2.17969796   -1.50063859   -0.82534174

H                  4.34210764    2.40496752    0.07853852

H                  6.80683188    2.17073421    0.03577112

H                  6.55987676   -1.97072848    0.10677182

H                  4.08852417   -1.90787553    0.25345561

H                 -4.34233462   -2.40779506   -0.08452701

H                 -6.80694163   -2.17375189   -0.04010162

H                 -6.56029497    1.96779835   -0.10652144

H                 -4.08907976    1.90527250   -0.25513532

H                  8.32713875   -1.30388925    1.72093878

H                 10.79096775   -1.47264986    1.60246204

H                 10.81717943    1.15342882   -1.79808171

H                  8.34923169    1.29336980   -1.71470098

H                 -8.32842105    1.29692984   -1.72402299

H                -10.79266424    1.45957705   -1.60968252

H                -10.81826314   -1.17275100    1.78608572

H                 -8.34963402   -1.30623164    1.70714776

H                 12.85733696   -1.18177330    0.26476317

H                 12.86481339   -0.12944415   -1.16645251

H                 12.93267312    0.57339595    0.45220092

H                -12.92707310    0.41191485   -0.81543009

H                -12.93230725   -0.61128064    0.63667064

H                -12.77682889    1.14257733    0.78496637

Cartesian coordinates of optimized dimer structure of compound G1, ground state

C                 -2.14840301    1.86063354   -0.44741883

C                 -1.44586387    1.33814178    0.68408018

C                 -2.19426461    0.79917759    1.76534099

C                 -3.56643267    0.80408410    1.74290663

C                 -4.27491539    1.35191123    0.63307094

C                 -3.56121799    1.86031297   -0.44290821

C                 -1.39967246    2.35794062   -1.54805338

C                 -0.02913562    2.37379479   -1.51398971

C                  0.68179675    1.90320676   -0.36946862

C                 -0.03337096    1.37805255    0.69766563

C                  2.14868709    2.00629106   -0.31595923

C                 -5.74655229    1.37218134    0.63259940

C                  2.85223126    2.92505215   -1.11915142

C                  4.22347304    3.01236160   -1.05746374

N                  4.94301563    2.19978560   -0.23824935

C                  4.29467358    1.31195072    0.56224586

C                  2.92342203    1.21311836    0.55014163

C                 -6.48055971    1.45695142    1.83013696

C                 -7.85714002    1.46141400    1.81126880

N                 -8.54175118    1.34646775    0.64305897

C                 -7.86431524    1.26000657   -0.53201833

C                 -6.48930156    1.29284449   -0.55968533

C                  6.38694217    2.26596659   -0.23643957

C                 -9.98504371    1.28352574    0.64827601

C                  7.08604119    2.14486006    0.96420718

C                  8.47849027    2.17388232    0.94289834

C                  9.18763837    2.34345969   -0.25383214

C                  8.45555075    2.47475041   -1.44359192

C                  7.06491760    2.42897256   -1.44648121

C                -10.70688577    1.96375961   -0.33253234

C                -12.09456849    1.85579481   -0.34645287

C                -12.77601411    1.08997930    0.60982114

C                -12.02309898    0.42997811    1.59053141

C                -10.63490539    0.51861742    1.61756005

C                 10.69270684    2.39564823   -0.26656651

C                -14.27965200    0.99975531    0.59928313

H                 -1.66468908    0.37501244    2.61249904

H                 -4.11558438    0.36095056    2.56589963

H                 -4.07685490    2.29656490   -1.29222354

H                 -1.92857664    2.72393251   -2.42245052

H                  0.51581560    2.73397698   -2.37843073

H                  0.47425790    1.01962557    1.58592418

H                  2.33592652    3.61298571   -1.77475236

H                  4.78527003    3.73671933   -1.62928640

H                  4.91449911    0.67658218    1.17723800

H                  2.46961747    0.47260367    1.19234739

H                 -5.98527695    1.56313516    2.78646068

H                 -8.45207310    1.57671323    2.70606183

H                 -8.45949291    1.12747896   -1.42345861

H                 -6.00412783    1.21324475   -1.52315684

H                  6.56003901    2.05150550    1.90769963

H                  9.02132902    2.07573485    1.87730983

H                  8.98042457    2.59134844   -2.38693860

H                  6.52266676    2.47891745   -2.38421786

H                -10.20099195    2.58611241   -1.06240043

H                -12.65636047    2.38544663   -1.10959620

H                -12.52626605   -0.17856847    2.33544480

H                -10.07134929   -0.02929423    2.36424158

H                 11.11253384    1.97967387    0.65212133

H                 11.09942273    1.83523350   -1.11358647

H                 11.04161028    3.43138179   -0.35995932

H                -14.67766579    1.11066846   -0.41349909

H                -14.62300766    0.04431660    1.00660767

H                -14.71780061    1.79591793    1.21442460

C                  1.55161344   -1.80317688   -0.94093699

C                  2.11175728   -2.08728227    0.34462225

C                  1.23498962   -2.31302440    1.44093059

C                 -0.12518641   -2.29258490    1.26642343

C                 -0.69281944   -2.03916522   -0.01730486

C                  0.14711928   -1.78718173   -1.09221831

C                  2.43010273   -1.55090948   -2.02910683

C                  3.79026569   -1.56502343   -1.85347193

C                  4.35979873   -1.83604541   -0.57405166

C                  3.51624654   -2.10161897    0.49626345

C                  5.81569242   -1.75584801   -0.36873888

C                 -2.15140318   -2.06283021   -0.19736320

C                  6.63669716   -1.00689259   -1.23223958

C                  7.97975404   -0.85677910   -0.97198312

N                  8.54871177   -1.43398886    0.11549989

C                  7.79758356   -2.20185875    0.94813168

C                  6.45100394   -2.37483649    0.72631715

C                 -2.98375495   -2.81776458    0.65101150

C                 -4.34680851   -2.83131085    0.47052867

N                 -4.92961129   -2.10093265   -0.51787695

C                 -4.15306997   -1.37036637   -1.36165052

C                 -2.78489332   -1.34556193   -1.22838673

C                  9.94421017   -1.19742211    0.40571459

C                 -6.36864856   -2.07984147   -0.65161127

C                 10.31229719   -0.80941965    1.69345904

C                 11.65522294   -0.56126577    1.96280558

C                 12.63229624   -0.68566342    0.96488194

C                 12.22845208   -1.08270273   -0.31736263

C                 10.89143359   -1.34124756   -0.60652617

C                 -6.94603529   -2.11051431   -1.92177626

C                 -8.33150599   -2.05259280   -2.03661105

C                 -9.15665748   -1.98934465   -0.90382888

C                 -8.54604117   -1.98580460    0.35747047

C                 -7.16106080   -2.01506035    0.49458513

C                 14.07647652   -0.37079011    1.25656879

C                -10.65444865   -1.90998948   -1.04536740

H                  1.65681532   -2.49957449    2.42354251

H                 -0.77276649   -2.44572788    2.12201078

H                 -0.25819141   -1.60782027   -2.08207039

H                  2.00928424   -1.34727156   -3.00870919

H                  4.43469000   -1.38778419   -2.70626462

H                  3.91675942   -2.27410890    1.48928876

H                  6.23033137   -0.48584583   -2.08819361

H                  8.62553502   -0.24126177   -1.57973219

H                  8.32224693   -2.67124092    1.76849140

H                  5.90604758   -3.01454841    1.40753045

H                 -2.57224142   -3.43315555    1.43975875

H                 -5.00911370   -3.43143122    1.07735603

H                 -4.67010796   -0.79765088   -2.11720566

H                 -2.22322017   -0.71676649   -1.90545566

H                  9.56170805   -0.67527858    2.46488973

H                 11.94488446   -0.25253173    2.96253106

H                 12.97061825   -1.20208778   -1.10061987

H                 10.59572616   -1.67496921   -1.59543476

H                 -6.33010615   -2.20334318   -2.80946090

H                 -8.77928329   -2.07744254   -3.02517776

H                 -9.16127100   -1.94931345    1.24966633

H                 -6.71201316   -1.95881480    1.47985736

H                 14.32775639   -0.58272722    2.29994975

H                 14.74742416   -0.94606995    0.61203833

H                 14.28074984    0.69264030    1.07848355

H                -11.00983165   -2.57065330   -1.84225654

H                -11.15788761   -2.18183486   -0.11455432

H                -10.96601233   -0.89057205   -1.30280364

Cartesian coordinates of optimized CB[7]⸱G1, ground state

C                  0.31059814    0.66316554    0.18697326

C                 -0.50110085   -0.48663510    0.45457222

C                  0.10934508   -1.64201451    1.01478989

C                  1.45915281   -1.67517386    1.26383351

C                  2.27104406   -0.53548306    0.98609207

C                  1.69128087    0.61331693    0.47077006

C                 -0.28721251    1.81325091   -0.39031970

C                 -1.62457057    1.83134560   -0.69001490

C                 -2.44230376    0.69657371   -0.41817460

C                 -1.87831438   -0.44078169    0.14126088

C                 -3.87708021    0.74373468   -0.72851028

C                  3.72424792   -0.56979820    1.18770514

C                 -4.58724332    1.95801797   -0.67320278

C                 -5.93512756    1.98198410   -0.94608265

N                 -6.59833768    0.84583836   -1.29137777

C                 -5.93384785   -0.33797207   -1.36702054

C                 -4.58948587   -0.41466245   -1.08693640

C                  4.45216807   -1.76382150    1.03440182

C                  5.82282858   -1.75635092    1.15267072

N                  6.49270226   -0.60902214    1.44100884

C                  5.81207914    0.55500009    1.61956233

C                  4.44320297    0.60050830    1.49937076

C                 -8.01454232    0.89466921   -1.57236270

C                  7.93339605   -0.62409827    1.54822801

C                 -8.86676164   -0.01330141   -0.94508282

C                -10.23054121    0.04087291   -1.22016027

C                -10.75637522    0.98939068   -2.10823940

C                 -9.87386013    1.89224396   -2.71703511

C                 -8.50588064    1.85050656   -2.46026823

C                  8.68106530    0.30995166    0.83257572

C                 10.06868118    0.29197665    0.94642951

C                 10.72007509   -0.64889225    1.75601173

C                  9.93904524   -1.57410979    2.46225731

C                  8.54985950   -1.56892265    2.36705395

C                -12.23100531    1.02198853   -2.41940570

C                 12.22456014   -0.68051930    1.84564151

H                 -0.51162301   -2.50373999    1.23982830

H                  1.89472560   -2.56692932    1.69863599

H                  2.30530542    1.47549428    0.23252670

H                  0.33261799    2.67853515   -0.59918414

H                 -2.05051698    2.70632212   -1.16090050

H                 -2.49540466   -1.30450350    0.35905250

H                 -4.10189241    2.87350299   -0.35666614

H                 -6.53666943    2.87732896   -0.87185032

H                 -6.51972517   -1.19174519   -1.67837419

H                 -4.10205482   -1.37863468   -1.17023920

H                  3.96126472   -2.68246541    0.74081866

H                  6.43324613   -2.63402323    0.99033520

H                  6.40878232    1.41854274    1.87903517

H                  3.94265866    1.54756034    1.66449134

H                 -8.47491604   -0.73149370   -0.23243680

H                -10.89777731   -0.65839802   -0.72518394

H                -10.25922177    2.63380778   -3.41043077

H                 -7.82943627    2.53713522   -2.95831042

H                  8.18889923    1.02489342    0.18149040

H                 10.65428132    1.01623592    0.38811226

H                 10.42194806   -2.30219118    3.10711790

H                  7.95374429   -2.27020251    2.94153129

H                -12.82489205    0.67155031   -1.56993717

H                -12.56051139    2.03191478   -2.68096582

H                -12.46141014    0.37027350   -3.27182460

H                 12.65312423    0.31574881    1.70153062

H                 12.55750042   -1.06542035    2.81414675

H                 12.64497707   -1.33397073    1.07060882

N                  0.56571228    5.04246135   -1.82277899

C                  1.98916446    5.33190127   -1.91272506

H                  2.15016753    6.40485561   -2.05879742

N                  2.79793840    4.84240770   -0.82104620

C                  0.12096405    4.27466838   -2.88766740

O                 -1.04387053    3.99048769   -3.13176263

C                  3.57830201    3.75948446   -1.16742948

O                  4.36082205    3.16965482   -0.43375820

N                  1.22095178    3.91885239   -3.63770901

C                  2.45803009    4.45552084   -3.11792228

H                  2.98735787    5.01804147   -3.89408582

N                  3.34780290    3.48633024   -2.50154999

C                  1.11229760    3.15879853   -4.85847165

H                  0.06653264    3.18562560   -5.16366886

H                  1.73407791    3.63608099   -5.62461074

C                  4.25898529    2.64809758   -3.25067406

H                  5.08201048    2.39290976   -2.58344553

H                  4.63725713    3.21119685   -4.11149696

N                  1.48815750    1.76536894   -4.74013045

C                  2.85976080    1.30651825   -4.89765160

H                  3.33337309    1.80836473   -5.74845076

N                  3.68850031    1.41472395   -3.72275559

C                  0.57026855    0.76215005   -5.01276865

O                 -0.64148329    0.89845669   -5.09891810

C                  3.91265703    0.20048959   -3.10496469

O                  4.58000979    0.01079177   -2.09759689

N                  1.27624944   -0.40745050   -5.21357952

C                  2.70239045   -0.23279792   -5.08138217

H                  3.22099547   -0.62949197   -5.96095951

N                  3.28381436   -0.77324921   -3.86318154

C                  0.64932995   -1.62767874   -5.66017569

H                  1.22353564   -2.02731553   -6.50354092

H                 -0.35888380   -1.37338787   -5.98609373

C                  3.64643885   -2.16413136   -3.72189244

H                  4.39953718   -2.22451904   -2.93624676

H                  4.06908402   -2.52481385   -4.66888537

N                  0.52669611   -2.65581092   -4.65420167

C                  1.59218481   -3.55782667   -4.28337519

H                  2.10454623   -3.93315925   -5.17594250

N                  2.55386510   -3.02452682   -3.33478601

C                 -0.69359545   -3.01939013   -4.11921321

O                 -1.76383685   -2.46266661   -4.31655750

C                  2.59455459   -3.75058763   -2.16054920

O                  3.39392655   -3.59649015   -1.24548842

N                 -0.49246516   -4.15584299   -3.35505201

C                  0.86149707   -4.66582571   -3.46293913

H                  0.86263878   -5.64884881   -3.94596240

N                  1.60890509   -4.71213369   -2.22730409

C                 -1.60437962   -4.95533870   -2.89767718

H                 -2.51026422   -4.50888683   -3.30720292

H                 -1.49445440   -5.97943018   -3.27179192

C                  1.44479589   -5.72493413   -1.21542907

H                  2.35612095   -5.74115859   -0.61813375

H                  1.30612903   -6.69362414   -1.70861336

N                 -1.75880170   -5.00472362   -1.46408543

C                 -1.02321700   -5.88911094   -0.58825851

H                 -1.05367199   -6.91544847   -0.96869376

N                  0.34503045   -5.49330859   -0.30589306

C                 -2.71137393   -4.26453068   -0.80155803

O                 -3.48297643   -3.45976405   -1.31068610

C                  0.56396849   -5.26780461    1.03976502

O                  1.64521212   -5.04305011    1.56779948

N                 -2.67359351   -4.62258929    0.53255412

C                 -1.73650813   -5.70343868    0.78758333

H                 -2.26976567   -6.59489184    1.13343174

N                 -0.65134801   -5.38099839    1.68533722

C                 -3.76151608   -4.29353604    1.42619499

H                 -4.54638850   -3.82664809    0.83117755

H                 -4.14033736   -5.21689881    1.88126189

C                 -0.78206578   -5.27669025    3.11977060

H                  0.21925516   -5.36984180    3.53930769

H                 -1.41370713   -6.09630717    3.47777869

N                 -3.40111522   -3.35885786    2.46272320

C                 -2.74506938   -3.74442495    3.69862723

H                 -3.26862759   -4.58701663    4.16285931

N                 -1.33213719   -4.02686598    3.58972988

C                 -3.97041153   -2.10221137    2.53293883

O                 -4.69170814   -1.58980277    1.68677032

C                 -0.54639829   -3.04940313    4.17124699

O                  0.67180692   -3.06687185    4.27132867

N                 -3.60604262   -1.54400669    3.73904072

C                 -2.79218295   -2.43119439    4.54162679

H                 -3.23557712   -2.55825416    5.53498161

N                 -1.39181122   -2.06888220    4.65382438

C                 -4.14268588   -0.28148224    4.19137317

H                 -4.99516147   -0.04549391    3.55482129

H                 -4.47245343   -0.39387815    5.23019509

C                 -0.90949636   -1.03556553    5.53790886

H                  0.14648780   -1.23548990    5.71881567

H                 -1.46344418   -1.08099753    6.48375536

N                 -3.22759934    0.83186765    4.10803988

C                 -2.21263568    1.10528714    5.10164998

H                 -2.63612747    1.03396549    6.10939394

N                 -1.01506104    0.29796928    5.00027510

C                 -3.41062617    1.87737448    3.22380497

O                 -4.26445923    1.94354992    2.35093652

C                  0.10411553    1.03967672    4.67367551

O                  1.24986742    0.62086434    4.58638661

N                 -2.48333566    2.85813414    3.53405805

C                 -1.71783639    2.53577935    4.72456599

H                 -1.89508288    3.28453655    5.50428478

N                 -0.30158271    2.34966486    4.51336734

C                 -2.61658819    4.20697231    3.02770509

H                 -2.69729367    4.89862794    3.87468014

H                 -3.53000315    4.24287506    2.43453615

C                  0.63440287    3.43228293    4.38115282

H                  1.62814619    3.03021463    4.57681331

H                  0.39364585    4.20482130    5.12183021

N                 -1.53536224    4.64039746    2.17471865

C                 -0.24823942    5.08638108    2.66189726

H                 -0.37761204    5.81132221    3.47271221

N                  0.66644249    4.03434369    3.06701705

C                 -1.68958557    4.83876188    0.81933047

O                 -2.70664847    4.62969665    0.16704240

C                  1.83325521    4.03812095    2.32676608

O                  2.82157782    3.34743043    2.53906456

N                 -0.50456764    5.35476263    0.33311058

C                  0.43385874    5.68134966    1.39192882

H                  0.59134025    6.76398731    1.44076733

N                  1.70086612    4.99106043    1.33808615

C                 -0.36276930    5.81921224   -1.02684002

H                 -1.34340372    5.73906877   -1.49575972

H                 -0.03994323    6.86697139   -1.02130755

C                  2.81144987    5.39538608    0.50869634

H                  2.82196668    6.48802534    0.44267810

H                  3.72453242    5.04586382    0.98977314

Cartesian coordinates of optimized CB[8]⸱G12, ground state

C                 -0.48255304    1.66322261   -0.70722373

C                 -1.04806551    1.76168635    0.60260855

C                 -0.21992754    2.15843653    1.68536563

C                  1.11033539    2.41892229    1.49003952

C                  1.69058675    2.29676918    0.19318624

C                  0.89067246    1.93350584   -0.88270583

C                 -1.32498303    1.27914254   -1.78553162

C                 -2.66111673    1.04506028   -1.58635626

C                 -3.23741548    1.17358989   -0.28712151

C                 -2.41943348    1.49445366    0.78634632

C                 -4.68301993    1.03066034   -0.08815655

C                  3.12647275    2.53046060    0.00780727

C                 -5.58359649    1.13818182   -1.16619256

C                 -6.93764576    1.00289701   -0.96623295

N                 -7.44779581    0.79271442    0.27711221

C                 -6.60641600    0.71807793    1.34496589

C                 -5.24489507    0.81266907    1.18725958

C                  4.02113170    2.49492545    1.09637007

C                  5.37235042    2.65798642    0.89896731

N                  5.88014493    2.86571904   -0.34468849

C                  5.03877010    2.94049030   -1.41255366

C                  3.68231483    2.77896215   -1.26410808

C                 -8.86914569    0.61119005    0.45630593

C                  7.31033974    2.93849957   -0.54092062

C                 -9.33066540   -0.38754731    1.31233538

C                -10.70103715   -0.58400684    1.44913958

C                -11.62320904    0.19438287    0.73874430

C                -11.12986419    1.19204153   -0.11376632

C                 -9.76306682    1.41219258   -0.25515239

C                  7.89196576    2.18988414   -1.56518076

C                  9.27396141    2.21478037   -1.72205648

C                 10.08763139    2.97677946   -0.87304299

C                  9.47346468    3.72778863    0.13770337

C                  8.09148776    3.71709714    0.31157715

C                -13.10578044   -0.02234240    0.89910889

C                 11.58332691    2.98995868   -1.05082694

H                 -0.66426997    2.27871295    2.66652210

H                  1.70729167    2.76526085    2.32304335

H                  1.31266068    1.82377873   -1.87442030

H                 -0.89284479    1.16571708   -2.77439142

H                 -3.26931622    0.74707768   -2.43047238

H                 -2.82719652    1.60046306    1.78286319

H                 -5.23426813    1.35237507   -2.16670495

H                 -7.65213459    1.04130195   -1.77587877

H                 -7.07341968    0.58854187    2.31093926

H                 -4.63069468    0.73187765    2.07516834

H                  3.68055710    2.29365849    2.10418857

H                  6.08929928    2.59163773    1.70450734

H                  5.50022520    3.14915604   -2.36758501

H                  3.06595370    2.87049597   -2.14872058

H                 -8.63917060   -1.04029646    1.83066862

H                -11.05556362   -1.37758367    2.09942527

H                -11.82439832    1.81445382   -0.66978978

H                 -9.40243739    2.20960125   -0.89553438

H                  7.27856329    1.57119141   -2.21048495

H                  9.72751881    1.61090257   -2.50185210

H                 10.08367674    4.32962330    0.80409167

H                  7.63073323    4.31745623    1.08867422

H                -13.64271638    0.20212926   -0.02744007

H                -13.32721667   -1.05418831    1.18675898

H                -13.51159610    0.63257751    1.68053123

H                 12.09255434    3.24017068   -0.11588205

H                 11.94674701    2.01620905   -1.39171062

H                 11.87994277    3.73450500   -1.80028051

C                  1.04743170   -1.76231697    0.60294273

C                  0.48153565   -1.66472867   -0.70678649

C                  1.32367796   -1.28162613   -1.78564238

C                  2.65988693   -1.04735650   -1.58708085

C                  3.23650252   -1.17466486   -0.28788143

C                  2.41885252   -1.49495111    0.78603182

C                  0.21954112   -2.15813102    1.68622963

C                 -1.11088065   -2.41833585    1.49150241

C                 -1.69150137   -2.29698496    0.19472792

C                 -0.89179432   -1.93479793   -0.88168388

C                 -3.12748853   -2.53039609    0.00990136

C                  4.68210404   -1.03098273   -0.08923370

C                 -4.02192108   -2.49315522    1.09858486

C                 -5.37323652   -2.65601803    0.90170107

N                 -5.88136146   -2.86526136   -0.34156692

C                 -5.04024496   -2.94160539   -1.40952146

C                 -3.68371195   -2.78026808   -1.26158374

C                  5.58257386   -1.13913718   -1.16728036

C                  6.93661456   -1.00328911   -0.96757194

N                  7.44678577   -0.79192297    0.27555714

C                  6.60549433   -0.71635746    1.34339308

C                  5.24398292   -0.81140588    1.18590369

C                 -7.31160871   -2.93793901   -0.53736129

C                  8.86813157   -0.60990891    0.45452654

C                 -7.89332347   -2.19039999   -1.56236009

C                 -9.27535691   -2.21519756   -1.71888758

C                -10.08897232   -2.97609422   -0.86882368

C                 -9.47472412   -3.72603674    0.14265746

C                 -8.09270545   -3.71539583    0.31621816

C                  9.32938866    0.38993341    1.30935287

C                 10.69974209    0.58689190    1.44586151

C                 11.62204295   -0.19205322    0.73629766

C                 11.12892590   -1.19093140   -0.11495890

C                  9.76219654   -1.41161412   -0.25599032

C                -11.58469378   -2.98927794   -1.04636545

C                 13.10459926    0.02529918    0.89605775

H                  0.89124895   -1.16914260   -2.77447440

H                  3.26772695   -0.75027813   -2.43178159

H                  2.82694355   -1.60019329    1.78249806

H                  0.66421516   -2.27785523    2.66730858

H                 -1.70764106   -2.76395944    2.32496813

H                 -1.31403045   -1.82570823   -1.87335979

H                 -3.68106121   -2.29055380    2.10602008

H                 -6.08997652   -2.58829116    1.70730444

H                 -5.50197360   -3.15131818   -2.36419269

H                 -3.06759850   -2.87293804   -2.14623533

H                  5.23315444   -1.35430579   -2.16754690

H                  7.65109026   -1.04226130   -1.77720691

H                  7.07256167   -0.58557576    2.30917094

H                  4.62990324   -0.72953125    2.07379507

H                 -7.27993327   -1.57262654   -2.20855747

H                 -9.72898320   -1.61217691   -2.49930609

H                -10.08490533   -4.32699671    0.80986088

H                 -7.63186551   -4.31496689    1.09387332

H                  8.63772346    1.04308180    1.82694856

H                 11.05412088    1.38129521    2.09521028

H                 11.82362784   -1.81382418   -0.67023807

H                  9.40164649   -2.20988161   -0.89534744

H                -11.94819764   -2.01541315   -1.38684078

H                -11.88139568   -3.73352272   -1.79608696

H                -12.09375636   -3.23986491   -0.11143934

H                 13.51185905   -0.63264713    1.67417358

H                 13.64072906   -0.19480024   -0.03202821

H                 13.32544642    1.05611471    1.18777453

O                 -1.51823575   -5.54241412    2.13703071

O                  4.36403079   -3.67923317    1.75238666

O                 -2.29130596   -2.94715201    4.59028044

O                  3.37615730   -0.81649873    4.21037874

O                 -3.37294257    0.81813808    4.21200689

O                  2.29607852    2.94575732    4.58742630

O                 -4.36188926    3.68009255    1.75572642

O                  1.52114086    5.54187568    2.13365344

N                  0.58946026   -6.09159887    1.32356253

N                  0.41661404   -5.29439615    3.39816054

N                  2.95313033   -5.44033408    1.20607959

N                  2.70809184   -4.45240010    3.18774029

N                 -0.11177016   -3.60455962    5.05743994

N                 -0.75874778   -1.55420071    5.64804562

N                  2.14617954   -2.71132708    4.77191803

N                  1.54559185   -0.74439560    5.64154008

N                 -1.53997226    0.74484059    5.64013374

N                 -2.14262413    2.71257456    4.77387242

N                  0.76424519    1.55469446    5.64865153

N                  0.11659375    3.60368668    5.05425150

N                 -2.70440768    4.45335389    3.18929668

N                 -2.95089333    5.44045727    1.20735068

N                 -0.41242236    5.29500799    3.39691623

N                 -0.58720570    6.09191712    1.32243277

C                 -0.30499591   -5.62140039    2.26620118

C                  1.93212056   -6.23708954    1.85232649

H                  2.22467160   -7.29269211    1.86268148

C                  1.82310117   -5.60085841    3.27313372

H                  2.14215407   -6.26725143    4.08198187

C                  3.43675419   -4.43479528    2.01342296

C                 -0.23305454   -4.98291075    4.64684962

H                 -1.29513987   -5.19148253    4.52223821

H                  0.18281236   -5.62031848    5.43506432

C                  3.12326831   -3.68794667    4.33616834

H                  3.33912131   -4.36704106    5.17080425

H                  4.02853822   -3.14961919    4.05634071

C                 -1.17324105   -2.72518940    5.04123733

C                  1.06594747   -3.05285774    5.68433559

H                  1.42991893   -3.71818552    6.47394023

C                  0.58197866   -1.66584866    6.20007089

H                  0.55807097   -1.58277183    7.29155744

C                  2.45220856   -1.36067754    4.80427026

C                 -1.72831771   -0.59715591    6.13191699

H                 -2.70809453   -0.93807717    5.79878584

H                 -1.69762736   -0.57338493    7.22858456

C                  1.73362432    0.59775268    6.13293111

H                  2.71352676    0.93861991    5.80011730

H                  1.70251815    0.57419109    7.22956343

C                 -2.44826521    1.36190216    4.80515432

C                 -0.57675453    1.66629057    6.19964813

H                 -0.55367226    1.58289197    7.29113177

C                 -1.06040854    3.05347525    5.68396004

H                 -1.42214904    3.71969647    6.47384291

C                  1.17827829    2.72448593    5.03939415

C                 -3.11920087    3.68974892    4.33849808

H                 -3.33379202    4.36939860    5.17298305

H                 -4.02513790    3.15200777    4.05970434

C                  0.23853773    4.98225058    4.64454079

H                 -0.17576603    5.61953308    5.43370386

H                  1.30062743    5.19007393    4.51868748

C                 -3.43412805    4.43547304    2.01560964

C                 -1.81898604    5.60164408    3.27335565

H                 -2.13707007    6.26835730    4.08232019

C                 -1.92934115    6.23746034    1.85245525

H                 -2.22195754    7.29304443    1.86281464

C                  0.30806658    5.62147151    2.26413004

C                  3.56625017   -5.76358835   -0.05786426

H                  3.76317916   -6.84172953   -0.09217638

H                  4.50739297   -5.21649956   -0.11074250

C                  0.12698043   -6.78644167    0.14518979

H                 -0.95916232   -6.84473933    0.21234142

H                  0.55273584   -7.79646107    0.12816763

O                  1.64674732    5.21929778   -1.51061983

O                 -4.30258949    3.82431847   -2.04137821

O                  2.39292553    2.34699871   -4.18019998

O                 -3.56913774    1.22689507   -4.69506264

O                  3.56580191   -1.22818178   -4.69747143

O                 -2.39601550   -2.34791073   -4.17788387

O                  4.30176994   -3.82508600   -2.04451002

O                 -1.64702561   -5.21930804   -1.50734364

N                 -0.45070724    6.12803802   -1.09418688

N                 -0.12200727    5.04185795   -3.00992609

N                 -2.78383222    5.38041328   -1.21222102

N                 -2.50958388    4.61183468   -3.29171767

N                  0.34334579    3.33974151   -4.66082436

N                  0.89012894    1.43978416   -5.69572825

N                 -2.04808908    2.95538427   -5.01368910

N                 -1.49531528    0.90749566   -5.70005782

N                  1.49113524   -0.90896165   -5.70079708

N                  2.04439399   -2.95671665   -5.01439094

N                 -0.89435002   -1.44127906   -5.69488215

N                 -0.34676160   -3.34078872   -4.65959458

N                  2.50786017   -4.61332472   -3.29306366

N                  2.78358898   -5.38068337   -1.21332596

N                  0.12035500   -5.04210717   -3.00836349

N                  0.45062680   -6.12847443   -1.09295160

C                  0.48354524    5.42740755   -1.82675048

C                 -1.72953832    6.22366569   -1.75421439

H                 -2.06065281    7.26703902   -1.79688843

C                 -1.45834345    5.59155960   -3.15067147

H                 -1.49274343    6.31163061   -3.97590800

C                 -3.30172626    4.51670461   -2.16371067

C                  0.67095250    4.65079137   -4.14530853

H                  1.71232831    4.63141049   -3.82596101

H                  0.54612108    5.38779075   -4.95013650

C                 -2.89267607    4.03517870   -4.55762267

H                 -2.89428116    4.82404087   -5.31852589

H                 -3.89777769    3.63074139   -4.44234586

C                  1.31956086    2.36843273   -4.77453074

C                 -0.74309019    3.13767820   -5.60765665

H                 -0.76324910    3.94854434   -6.34317926

C                 -0.42319492    1.74084457   -6.21789004

H                 -0.41521972    1.72509015   -7.31261066

C                 -2.48763600    1.65155668   -5.08469013

C                  1.76123642    0.41420540   -6.21431312

H                  2.78095837    0.66643708   -5.92473733

H                  1.67796256    0.40861528   -7.30746319

C                 -1.76580650   -0.41578476   -6.21306500

H                 -2.78531303   -0.66793099   -5.92265729

H                 -1.68334571   -0.41047078   -7.30627572

C                  2.48395664   -1.65290150   -5.08607970

C                  0.41867366   -1.74243157   -6.21775198

H                  0.41002814   -1.72696651   -7.31247101

C                  0.73896326   -3.13908181   -5.60732782

H                  0.75850498   -3.95016787   -6.34262558

C                 -1.32311594   -2.36959782   -4.77305252

C                  2.88945793   -4.03659182   -4.55936295

H                  2.89010860   -4.82541185   -5.32031007

H                  3.89472475   -3.63223960   -4.44522931

C                 -0.67385489   -4.65157170   -4.14309770

H                 -0.54998465   -5.38898246   -4.94770315

H                 -1.71487618   -4.63196750   -3.82261394

C                  3.30082052   -4.51754631   -2.16571008

C                  1.45633722   -5.59247058   -3.15048672

H                  1.48943626   -6.31288016   -3.97548214

C                  1.72884754   -6.22418084   -1.75412012

H                  2.05999473   -7.26753724   -1.79682427

C                 -0.48417471   -5.42765203   -1.82460392

C                 -3.56529349    5.76354814   -0.05604177

H                 -3.76217161    6.84169736   -0.09032796

H                 -4.50652522    5.21651168   -0.10786037

C                 -0.12582672    6.78639754    0.14341409

H                  0.96038482    6.84462635    0.20949749

H                 -0.55152911    7.79643932    0.12652706

Cartesian coordinates of optimized CB[10]⸱G12, ground state

C                  4.04709954    0.15069740   -0.70703095

C                  4.06272768   -0.17117689    0.68848082

C                  4.00554428    0.88629587    1.63655355

C                  3.97071386    2.19245179    1.22429468

C                  4.05460413    2.52330121   -0.15928674

C                  4.08089366    1.50564390   -1.10187020

C                  3.97513184   -0.90715688   -1.65363077

C                  3.95555029   -2.21344371   -1.24055801

C                  4.07220778   -2.54374620    0.14072807

C                  4.11307167   -1.52576045    1.08261024

C                  4.14658755   -3.94849877    0.55969228

C                  4.10821725    3.92860791   -0.57932454

C                  3.62224956   -4.98768082   -0.23412265

C                  3.69207890   -6.29232432    0.19762981

N                  4.28216020   -6.60968547    1.38014696

C                  4.81647287   -5.63112433    2.15911430

C                  4.75720814   -4.31194796    1.77661883

C                  3.58984295    4.96076955    0.22708009

C                  3.64002045    6.26709955   -0.20177451

N                  4.20505712    6.59232866   -1.39444321

C                  4.73086019    5.62015835   -2.18733118

C                  4.69015153    4.29930157   -1.80788030

C                  4.34352578   -7.98759640    1.81092976

C                  4.24928534    7.97223158   -1.82098031

C                  3.91705762   -8.32033347    3.09603850

C                  3.97724414   -9.65045520    3.50279288

C                  4.45304928  -10.65250101    2.64567800

C                  4.86825408  -10.28546864    1.35824427

C                  4.82188784   -8.96000473    0.93399206

C                  3.79692166    8.30731921   -3.09659369

C                  3.84083342    9.63940932   -3.49895734

C                  4.32585927   10.64117910   -2.64672621

C                  4.76729311   10.27177359   -1.36872574

C                  4.73748763    8.94436225   -0.94912930

C                  4.53905346  -12.08524614    3.10617869

C                  4.39388743   12.07628970   -3.10279361

H                  3.96957886    0.65173224    2.69531793

H                  3.91500261    2.98177217    1.95913338

H                  4.10959496    1.72685288   -2.16307733

H                  3.91659551   -0.67299636   -2.71158146

H                  3.88598210   -3.00343112   -1.97336067

H                  4.16634688   -1.74592570    2.14312100

H                  3.13012099   -4.79527103   -1.18041305

H                  3.26666085   -7.11741945   -0.35673738

H                  5.30629438   -5.96019400    3.06518156

H                  5.23637518   -3.57138192    2.40354777

H                  3.11779262    4.75800351    1.18130767

H                  3.21878608    7.08719385    0.36310036

H                  5.19938676    5.95591698   -3.10217395

H                  5.16010545    3.56408788   -2.44820360

H                  3.51865692   -7.55798459    3.75726053

H                  3.63601813   -9.91433727    4.49932411

H                  5.24329147  -11.04488705    0.67876377

H                  5.17218467   -8.68472869   -0.05527394

H                  3.39130175    7.54502387   -3.75343753

H                  3.47943273    9.90494914   -4.48790596

H                  5.14987628   11.03095122   -0.69318805

H                  5.10793386    8.66755207    0.03233775

H                  3.75937475  -12.31512052    3.83854410

H                  4.44341685  -12.78005179    2.26656950

H                  5.50683023  -12.28010640    3.58559389

H                  3.60046553   12.30339252   -3.82111790

H                  4.30730047   12.76706112   -2.25888030

H                  5.35212542   12.28004782   -3.59743143

C                 -4.06729576    0.16802408   -0.68476072

C                 -4.05364476   -0.15418406    0.71068890

C                 -3.97952416    0.90290850    1.65786042

C                 -3.95510600    2.20914124    1.24531256

C                 -4.06850665    2.54023424   -0.13605489

C                 -4.11268241    1.52296593   -1.07849389

C                 -4.01222762   -0.88960340   -1.63274442

C                 -3.98134733   -2.19589871   -1.22049046

C                 -4.06749480   -2.52666013    0.16293374

C                 -4.09152303   -1.50891926    1.10541854

C                 -4.12645397   -3.93158964    0.58329675

C                 -4.13391480    3.94566694   -0.55376926

C                 -3.61302762   -4.96638148   -0.22288653

C                 -3.66825840   -6.27221072    0.20695925

N                 -4.23359965   -6.59428477    1.40033736

C                 -4.75491062   -5.61943724    2.19293908

C                 -4.70903087   -4.29906707    1.81253325

C                 -3.60199734    4.97881530    0.24261911

C                 -3.66099427    6.28485160   -0.18596709

N                 -4.24767978    6.60899775   -1.36853364

C                 -4.78948365    5.63632715   -2.14980012

C                 -4.74110023    4.31580950   -1.77014489

C                 -4.28126439   -7.97370042    1.82810059

C                 -4.29638219    7.98827274   -1.79659811

C                 -3.83292875   -8.30839005    3.10510960

C                 -3.88668123   -9.63910022    3.51108077

C                 -4.37271233  -10.64050768    2.65916936

C                 -4.81694098  -10.27047414    1.38218162

C                 -4.77736179   -8.94450031    0.95906316

C                 -3.87155539    8.31917071   -3.08261727

C                 -3.92580507    9.64976600   -3.48885722

C                 -4.38909448   10.65474726   -2.62849503

C                 -4.81003965   10.28845193   -1.34258763

C                 -4.76964630    8.96267253   -0.91892238

C                 -4.39453953  -12.08283975    3.09666960

C                 -4.41127638   12.09676236   -3.06698623

H                 -3.92318314    0.66811908    2.71576591

H                 -3.88495650    2.99848372    1.97885639

H                 -4.16426832    1.74405570   -2.13894679

H                 -3.97432864   -0.65509254   -2.69145623

H                 -3.92657401   -2.98518758   -1.95536158

H                 -4.12149550   -1.72985117    2.16661505

H                 -3.14055410   -4.76605356   -1.17742383

H                 -3.25094865   -7.09449591   -0.35766493

H                 -5.22397196   -5.95256094    3.10845590

H                 -5.17394272   -3.56103499    2.45336181

H                 -3.11286752    4.77663736    1.18829263

H                 -3.22962538    7.10557900    0.37030002

H                 -5.27617226    5.97117337   -3.05541493

H                 -5.22585220    3.57999240   -2.39838862

H                 -3.42964062   -7.54605873    3.76334734

H                 -3.53516685   -9.90328472    4.50394658

H                 -5.21242102  -11.02746029    0.71157095

H                 -5.15301656   -8.66625220   -0.02001149

H                 -3.48566536    7.55394284   -3.74792578

H                 -3.59263335    9.91097070   -4.48881380

H                 -5.18785141   11.04831898   -0.66509015

H                 -5.12747278    8.68752676    0.06767823

H                 -4.51986671  -12.16858107    4.18013576

H                 -5.20321042  -12.63456593    2.60821915

H                 -3.45236844  -12.58092472    2.83467148

H                 -4.56062684   12.18229835   -4.14742298

H                 -5.20493462   12.65432621   -2.56088079

H                 -3.46005776   12.58875215   -2.82709438

N                 -1.21335149    3.35912174    5.04301634

C                 -1.64712283    2.67451063    6.25890699

H                 -1.38009885    3.26199428    7.14460058

N                 -1.18575516    1.31482629    6.38805143

C                 -2.30757410    3.82152511    4.31555813

O                 -2.26082025    4.56461063    3.34298870

C                 -2.19697501    0.39082311    6.19752873

O                 -2.09588124   -0.82160084    6.31262081

N                 -3.45730666    3.32047220    4.89548691

C                 -3.17992632    2.52111276    6.06278475

H                 -3.76869933    2.87316941    6.91740616

N                 -3.35048141    1.09013452    5.87789085

C                 -4.76752146    3.87781881    4.64158790

H                 -5.17650670    4.24329368    5.59244338

H                 -4.65235538    4.71185863    3.94990373

C                 -4.64194157    0.45733706    6.02978996

H                 -5.12606926    0.82315598    6.94544531

H                 -4.46591064   -0.61455328    6.11284460

N                 -5.69621250    2.95116731    4.03647570

C                 -6.33496929    1.87042860    4.76796510

H                 -6.68586445    2.21944560    5.74543588

N                 -5.53271414    0.67429382    4.91702329

C                 -6.40202679    3.30254285    2.89876368

O                 -6.17271666    4.26636170    2.18054709

C                 -6.01398397   -0.38248870    4.16611966

O                 -5.55270318   -1.51859119    4.15018931

N                 -7.41776722    2.38561001    2.73726601

C                 -7.48399307    1.42329818    3.81315286

H                 -8.47555503    1.43548075    4.27789749

N                 -7.11207158    0.06320157    3.46186614

C                 -8.42835628    2.53260001    1.71673868

H                 -9.41784783    2.48985120    2.18417318

H                 -8.27832797    3.51044346    1.25996584

C                 -8.03569639   -0.86739682    2.85432546

H                 -7.69610647   -1.87485051    3.09261115

H                 -9.03307421   -0.70280427    3.28256987

N                 -8.37309012    1.54825142    0.66448837

C                 -8.94122376    0.22568291    0.75445596

H                 -9.93425889    0.26379657    1.21480361

N                 -8.10805794   -0.76488921    1.41812401

C                 -7.87720034    1.82790395   -0.59313808

O                 -7.35585597    2.87527461   -0.94934465

C                 -7.87281748   -1.87030636    0.61770676

O                 -7.34880193   -2.91794879    0.96908817

N                 -8.12098272    0.72313914   -1.39141463

C                 -8.94810200   -0.26727327   -0.72015707

H                 -9.94531599   -0.30516304   -1.17134236

N                 -8.37940500   -1.58988157   -0.63555536

C                 -8.05990381    0.82489093   -2.82815278

H                 -7.72437210    1.83295494   -3.06962491

H                 -9.06023953    0.65801611   -3.24845513

C                 -8.44346630   -2.57330819   -1.68822115

H                 -9.43617414   -2.52921737   -2.14846971

H                 -8.29114496   -3.55162378   -1.23319988

N                 -7.13881175   -0.10396501   -3.44197392

C                 -7.51090708   -1.46458680   -3.79167691

H                 -8.50381066   -1.47791934   -4.25343838

N                 -7.44036283   -2.42706616   -2.71619347

C                 -6.04626018    0.34430689   -4.15368587

O                 -5.58638663    1.48084866   -4.13976564

C                 -6.41829819   -3.33698699   -2.87597501

O                 -6.18153937   -4.29734927   -2.15545480

N                 -5.56901559   -0.71126209   -4.90882100

C                 -6.36402408   -1.91040872   -4.74968323

H                 -6.71746929   -2.26712761   -5.72344423

N                 -5.71533644   -2.98333542   -4.01480698

C                 -4.68461970   -0.49423460   -6.02648393

H                 -4.51533360    0.57825722   -6.11565310

H                 -5.17094946   -0.86739154   -6.93796840

C                 -4.78396483   -3.90758263   -4.61985687

H                 -5.19481493   -4.27975842   -5.56729672

H                 -4.66109001   -4.73770691   -3.92480293

N                 -3.38851946   -1.11849214   -5.87756969

C                 -3.21038586   -2.54971853   -6.05503024

H                 -3.80039450   -2.91032037   -6.90519582

N                 -3.47846464   -3.34381290   -4.88228379

C                 -2.24124178   -0.41456715   -6.20944807

O                 -2.14827635    0.79753026   -6.33454108

C                 -2.32351909   -3.83093234   -4.30115495

O                 -2.26832310   -4.56489098   -3.32223074

N                 -1.22607767   -1.33389699   -6.40038898

C                 -1.67760427   -2.69512185   -6.25592370

H                 -1.41016591   -3.28986015   -7.13660556

N                 -1.23450612   -3.36501557   -5.03487931

C                  0.02085306    0.97104731    7.09726092

H                  0.02473424   -0.10861692    7.24147479

H                  0.02028661    1.47322495    8.07467680

C                  0.00634849    4.14894534    5.03734022

H                  0.00646732    4.81386794    5.91481319

H                  0.00263579    4.75212533    4.13076646

N                  1.20964631   -3.35735539   -5.03950485

C                  1.64426477   -2.68415218   -6.26167178

H                  1.37811081   -3.28015952   -7.14189225

N                  1.18279848   -1.32598370   -6.40382948

C                  2.30366206   -3.81399972   -4.30785130

O                  2.25616500   -4.54563605   -3.32671336

C                  2.19219329   -0.39973493   -6.21523606

O                  2.09018236    0.81189310   -6.33792146

N                  3.45393193   -3.32048563   -4.89319584

C                  3.17669486   -2.52837088   -6.06525997

H                  3.76650122   -2.88449300   -6.91743760

N                  3.34516285   -1.09603895   -5.88782875

C                  4.76301721   -3.87913616   -4.63682525

H                  5.17091105   -4.24935714   -5.58631408

H                  4.64672240   -4.71015949   -3.94171742

C                  4.63649387   -0.46271730   -6.03719104

H                  5.12363186   -0.82947330   -6.95089562

H                  4.45988862    0.60891629   -6.12240032

N                  5.69342638   -2.95179035   -4.03567308

C                  6.32925655   -1.87183850   -4.77083527

H                  6.67963211   -2.22248568   -5.74791375

N                  5.52438606   -0.67779974   -4.92166015

C                  6.40371174   -3.30194959   -2.90047054

O                  6.17817783   -4.26569313   -2.18075618

C                  6.00169944    0.38013113   -4.16974524

O                  5.53640118    1.51462773   -4.15270393

N                  7.41929284   -2.38395163   -2.74357514

C                  7.47862192   -1.42046100   -3.81858644

H                  8.46905646   -1.42781462   -4.28584671

N                  7.10133039   -0.06218800   -3.46537978

C                  8.43028994   -2.52526105   -1.72285873

H                  9.41964285   -2.47901639   -2.19027093

H                  8.28429571   -3.50313835   -1.26483443

C                  8.02402814    0.87246023   -2.86225611

H                  7.68073101    1.87849669   -3.10121417

H                  9.02054981    0.70990270   -3.29331755

N                  8.37044249   -1.53951943   -0.67199073

C                  8.93662330   -0.21609514   -0.76347591

H                  9.92896500   -0.25312222   -1.22545173

N                  8.10110979    0.77258783   -1.42642572

C                  7.88280872   -1.82183585    0.58827769

O                  7.36693059   -2.87132238    0.94621550

C                  7.86272803    1.87697186   -0.62607609

O                  7.33505132    2.92288056   -0.97706238

N                  8.12493224   -0.71581719    1.38530384

C                  8.94535155    0.27787837    0.71089448

H                  9.94365179    0.32056562    1.15928761

N                  8.37072766    1.59799162    0.62697205

C                  8.06816512   -0.81628003    2.82231121

H                  7.73759073   -1.82555422    3.06563678

H                  9.06889983   -0.64487975    3.23967087

C                  8.43348983    2.58219834    1.67890844

H                  9.42724247    2.54178663    2.13730583

H                  8.27679113    3.55969683    1.22367021

N                  7.14507880    0.10904966    3.43828315

C                  7.51034594    1.47189404    3.78547617

H                  8.50393523    1.49125513    4.24551460

N                  7.43281798    2.43266415    2.70873367

C                  6.05246865   -0.34240990    4.14741288

O                  5.59643878   -1.48058282    4.13275329

C                  6.41008282    3.34122450    2.87204124

O                  6.16946423    4.30124227    2.15233027

N                  5.56913826    0.71205709    4.90039456

C                  6.36254609    1.91314284    4.74488250

H                  6.71547726    2.26718441    5.71978597

N                  5.71221551    2.98710627    4.01363788

C                  4.68519862    0.49104046    6.01790221

H                  4.51757938   -0.58194004    6.10443465

H                  5.17096566    0.86274345    6.93028078

C                  4.77892639    3.90786774    4.62048229

H                  5.18863663    4.27787239    5.56925563

H                  4.65496140    4.73970753    3.92768832

N                  3.38835718    1.11369174    5.87084353

C                  3.20713669    2.54378660    6.05141082

H                  3.79642541    2.90366773    6.90237383

N                  3.47397252    3.34112345    4.88030463

C                  2.24091443    0.40620598    6.19329838

O                  2.14962901   -0.80663981    6.31255948

C                  2.31849874    3.83349528    4.30428546

O                  2.26263165    4.57310837    3.32952695

N                  1.22318221    1.32291167    6.38487933

C                  1.67388622    2.68590912    6.25272800

H                  1.40560903    3.27253071    7.13859220

N                  1.23042005    3.36595752    5.03782465

C                 -0.02375122   -0.98796441   -7.11552743

H                 -0.02753584    0.09051882   -7.26845272

H                 -0.02349007   -1.49799051   -8.08879969

C                 -0.00992220   -4.14744480   -5.02792473

H                 -0.00937250   -4.81911937   -5.90027627

H                 -0.00636990   -4.74359304   -4.11671589